Supporting Information

Interface-Engineered MXene/Layered Double Hydroxide Heterostructure

for Dopamine Sensing

Ayush Gadpayle,1,5,6 Hemil Marviya,1 Yi Yang,1 , Jean G. A. Ruthes,5,6  Peter Rolf Burger,5,6 Krutarth Kamath,1 Volker Presser,5,6,7 Babak Anasori,1,3 Arun Kumar Mannodi1 and Lia Stanciu1,2,4*

- School of Materials Engineering, Purdue University, 701 West Stadium Ave., West Lafayette, IN, 47907, USA

- School of Biomedical Engineering, Purdue University, 206 S Martin Jischke Dr, West Lafayette, IN, 47907, USA

- School of Mechanical Engineering, Purdue University, 701 West Stadium Ave., West Lafayette, IN, 47907, USA

- Bindley Bioscience Center, Purdue University, 1203 W State St, West Lafayette, IN, 47907, USA

- INM - Leibniz Institute for New Materials, D2 2, 66123, Saarbrücken, Germany

- Department of Materials Science & Engineering, Saarland University, Campus D2 2, 66123, Saarbrücken, Germany

- saarene, Saarland Center for Energy Materials and Sustainability, Campus C4 2, 66123 Saarbrücken, Germany

*	Corresponding authors’ email: lstanciu@purdue.edu (L. Stanciu)

Figure S1. EDX elemental spectrum of NFM-MX.

Figure S2: Schematic of atomic models of (A) Ti3C2Tx MXene (MX) (B) Ni2FeMn-LDH (NFM)  (C) NFM-MX

Figure S3. ELF plot of (a) Ti3C2Tx (MX), (b) Ni2FeMn-LDH (NFM)

Figure S4.  PDOS of NFM-MX

Figure S5. DPV plot of  (A) Bare SPE (B) MX (C) NFM

Figure S6. Schematics of atomic models of (A) DA-O2 (B) Ti3C2F2  (C) Ti3C2O2 (D) Ti3C2(OH)2 (E) Ti3C2Tx

Figure S7: Optimized adsorption configuration of DAO2 on the NFM-LDH bridge site obtained from DFT calculations. Dopamine exhibits strong adsorption with an adsorption energy of −1.34 eV, accompanied by elongation of the catechol O-H bond to 1.51 Å, indicating proton transfer and formation of a catecholate-like dopamine species. The elongated metal–oxygen distance reflects local surface coordination rearrangement during adsorption.

Figure S8. DPV response of (A) UA only  and (B) AA only